## Slide 1: MIT 3.156/3.46 Photonic Materials and Devices 4: Fiber Optics
Juejun (JJ) Hu
hujuejun@mit.edu

## Slide 2: Optical fibers
Cylindrical waveguide
(Typically) made of glasses
Low index contrast
Large core size
Single-mode fiber core
1 μm
Silicon waveguide

## Slide 3: Standard single-mode silica optical fiber structure
Core/cladding: low loss light propagation
Buffer/jacket: protection against mechanical damage and the environment (UV radiation, humidity, etc.)
Core
Cladding

## Slide 4: Linearly polarized (LP) fiber modes
Solutions to the Helmholtz equation in a cylindrical coordinate system
QM analog: 2-D hydrogen atom
  m : principal quantum number
  l : angular quantum number
Radial function
Angular function
Radial index m
Angular index l
www.rp-photonics.com/lp_modes.html

## Slide 5: Linearly polarized (LP) fiber modes
Radial index m
Angular index l

## Slide 6: Numerical aperture (NA)
Δn = ncore – nclad << 1, typical Δn = 0.001 ~ 0.02
Numerical Aperture
  Light gathering power θa
  For a silica fiber with ncore = 1.44 & nclad = 1.46, θa = 11.9º, NA = 0.209

## Slide 7: Single-mode step-index fiber design: V-parameter
V-parameter (V-number)
  Single-mode condition: V < 2.405
  Δn = 0.003, single-mode fiber dcore ~ 10 μm
Number of modes M
  M ~ 4V2/p2 ~ 0.4V2
v

## Slide 8: Optical fiber materials
Glasses: silica and other oxides, chalcogenides, halides, polymers
Metals, crystalline oxides and semiconductors, etc.
Dopants in silica glass
  Increase index: GeO2, P2O5, TiO2
  Decrease index: B2O3
  Luminescent centers: rare earth (e.g. Er)
Refractive index nD of SiO2-GeO2 glass
Appl. Opt. 24, 4486 (2004)

## Slide 9: Fiber drawing process
Fiber preforms
Drawing tower
Fiber spool
Viscosity window for fiber drawing:
104 to 106 Pa·s
Notes: https://www.technologyreview.com/s/401266/drawing-optical-fibers/

## Slide 10: Multi-material, microstructured optical fibers
Microstructured optical fibers: photonic bandgaps and various sizes of the rings give rise to the different colors
A. Argyros, the University of Sydney
Optical mode shaping
Dispersion engineering
Broadband transmission
Multi-functional sensing
Nat. Mater. 6, 336, (2007)

## Slide 11: Multi-material, microstructured optical fibers
Hollow-core photonic crystal fiber fabrication process flow using the stack-and-draw technique
Optical mode shaping
Dispersion engineering
Broadband transmission
Multi-functional sensing
Nat. Mater. 6, 336, (2007)
Nanophotonics 2, 315-340 (2013)
Notes: (A) Primary preform obtained by assembling a few hundred high purity, low-hydroxyl silica glass capillaries into an array with the required geometry tightly packed inside a glass tube; (B) first stage draw of the primary preform into a ~millimetre sized “cane”; (C) optical image of the cross-section of a HC-PBGF cane showing elimination of interstitial volumes and formation of the central core “defect”; (D) scanning electron microscope image of the microstructured region of the final fibre, showing a much increased diameter to pitch ratio of the cladding holes. The typical hole-to-hole spacing for operation at 1500 nm wavelength is in the range of 4–6 µm (depending on the air filling ratio of the cladding).

## Slide 12: Multi-material, microstructured optical fibers
Rod-in-tube
Extrusion
Stack-and-draw
Adv. Mater. 18, 845 (2006)
Int. J. Appl. Glass Sci. 3, 349 (2012)

## Slide 13: Multi-material, microstructured optical fibers
Adv. Mater. 18, 845 (2006)
Thermal sensing fibers

## Slide 14: Multi-material, microstructured optical fibers
Nat. Biotechnol. 33, 277 (2017)
Multifunctional fibers for simultaneous optical, electrical and chemical interrogation of neural circuits

## Slide 15: List of symbols
E – electric field
r – radial coordinate
j – angular coordinate
m – radial modal index
l – angular modal index
dcore – diameter of fiber core
ncore / nclad – refractive index of fiber core / cladding
NA – numerical aperture
qa – acceptance angle
V – V-parameter, V-number