## Slide 1: MIT 3.071 Amorphous Materials 1: Fundamentals of the Amorphous State
Juejun (JJ) Hu
hujuejun@mit.edu

## Slide 2: Contact Information
Juejun (JJ) Hu, Rm 13-4054
hujuejun@mit.edu
Ph: (302) 766-3083
Research interests
  We work with light
  Optics & photonics
  Novel optical materials (including amorphous materials)
  Chem-bio sensing, flexible optoelectronics, optical imaging, biomedical optics, photovoltaics, magneto-optics, data communications, …

## Slide 3: References
Fundamentals of Inorganic Glasses
  Arun K. Varshneya, Academic Press (1994)
  Google Books, MIT Library
Introduction to Glass Science and Technology
  James E. Shelby, Royal Society of Chemistry (2005)
  RSC Publishing (paste link to a browser window), MIT Library
Glass Science, 2nd Edition
  Robert H. Doremus, Wiley (1994)
  MIT Library
Springer Handbook of Glass
  J. D. Musgraves, J. Hu, L. Calvez (Eds.), Springer (2018)

## Slide 4: Class organization
Modules
  Lectures: MW 2:30-4 (4-153)
  Guest Lectures
  In-class demos
  MIT Glass lab: special thanks to Peter Houk & Prof. Cima
  Final project presentation
  2-3 individual project meetings
Stellar site
  Syllabus, announcements, lecture slides, assignments, solutions will be posted on Stellar
  Fall 2017 Stellar Link

## Slide 5: Grading policy
In-class quizzes: 10%
Homework assignments: 30%
  Discussions are allowed and encouraged; but you are supposed to complete the assignments independently
Design review project: 60%
  Project proposal: 20%
  Term paper: 25%
  Final presentation: 15%

## Slide 6: Important dates
Nov. 6 project proposal due
  Page limit: 5 (including figures & tables, excluding references); Font: Times New Roman 12; Page format: letter size with 1 inch margin
  Motivation and significance; Brief review of state-of-the-art; Proposed technical approach; Anticipated outcome
  1 executive summary slide
Dec. 11/13 project presentation
  Time limit and format: TBD

## Slide 7: Important dates
Dec. 15 term paper due
  Page limit: 8 (including figures & tables, excluding references); Font: Times New Roman 12; Page format: letter size with 1 inch margin
  Motivation and significance; Current state-of-the-art; Research methodology; Results and discussion; Conclusions
Document templates/examples will be posted on Stellar

## Slide 8: Project topic examples
Glass box cracks at 1,353 feet above: is it still safe?
Can we make smart phones smarter with built-in photonics?
Opt. Express 22, 15473 (2014).
Where is my metallic glass cased iPhone?
Are smart windows technologically and economically viable?

## Slide 9: Evaluation criteria
Proposals and papers
  Intellectual merit (75%): soundness, depth, thoroughness, inventiveness
  Presentation (25%): logical coherence, clarity, conciseness
In-class presentation
  Timing (20%)
  Presentation (40%): logical coherence, clarity, conciseness
  Intellectual merit (40%): soundness, depth, thoroughness, inventiveness

## Slide 10: What is glass (amorphous solid)?

## Slide 13: What is glass (amorphous solid)?
Mechanical properties
  Brittle, fragile, stiff
Optical properties
  Transparent, translucent
“A room-temperature malleable glass” (As60Se40)
Video courtesy of IRradiance Glass Inc.

## Slide 14: What is glass (amorphous solid)?
Electrical properties
  Insulating
Chemical properties
  Durable, inert
NASA: Galileo Spacecraft found amorphous ice on moons of Jupiter
Man-made
  Obsidian (volcanic activity)
  Tektite (meteorite impact)
  Fulgurite (lightning strike)
Metallic glass

## Slide 15: Amorphous materials are ubiquitous
Glass cover
Camera lens
TFT display
Dielectrics
Circuit packaging
Metallic glass case
Phase change memory
Solid state battery
and many more…

## Slide 16: What is amorphous solid (glass)?
A metastable solid with no long-range atomic order (and exhibiting glass transition)
metastable
E
Structure
Metastable glassy state
Thermodynamically stable crystalline state
Glasses are metastable with respect to their stable crystalline phase
Atoms can rearrange to form a more stable state given enough time and thermal energy

## Slide 17: What is amorphous solid (glass)?
A metastable solid with no long-range atomic order (and exhibiting glass transition)
no long-range atomic order
A2O3 crystal
A2O3 glass
Short-range order is preserved (AO3 triangles)
Long-range order is disrupted by changing bond angle (mainly) and bond length
Structure lacks symmetry and is usually isotropic
Zachariasen's Random Network Theory (1932)
Consider a fictitious A2O3 2-D compound:
Notes: Amorphous does not mean random

## Slide 18: Glass consists of a continuous atomic network
Absence of small angle scattering
  Continuous structure without micro-voids
Broad diffraction peak
  Size of ordered region < 8 Å (Scherrer equation)
  Unit cell size of cristobalite: 7.1 Å
Glass is NOT a collection of extremely small crystals
J. Am. Cer. Soc. 21, 49-54 (1938).

## Slide 19: Random network model of silica glass (SiO2)
Nature 212, 1353 (1966).
Now in the Science Museum, London
Excellent agreement between XRD and ball-and-stick model constructed according to the random network model
Radial distribution function

## Slide 20: Direct atomic imaging of bilayer silica glass
O
Si
Si-O tetrahedron
O
O
O
2-D projection
Quartz crystal
Si

## Slide 21: Direct atomic imaging of bilayer silica glass
Sci. Rep. 3, 3482 (2013).
Nano Lett. 12, 1081-1086 (2012).
STEM images of 2-D silica crystal and glass

## Slide 22: Glass formation from liquid
V, H
T
Tm
When the system is kept in thermal equilibrium:
First-order liquid-solid phase transition
Discontinuity of extensive thermo-dynamic parameters (e.g., V and H)
Reversible process
Liquid
Crystal
Melting / solidification
Notes: The enthalpy plot is generic but the V-T is not: note volume anomaly in silica glass

## Slide 23: Glass formation from liquid
T
Tm
Supercooled liquid
Glass transition
Glass
Crystal
Tf
Supercooled liquid transforms to the glassy state when crystallization is kinetically suppressed
Extensive variables remain continuous during glass transition
The glassy state is different from super-cooled liquid
Tf : Fictive temperature
Liquid
V, H
Notes: Slope change between liquid and solid: heat capacity or thermal expansion coefficient change

## Slide 24: Glass formation from liquid
V, H
T
Tm
Supercooled liquid
Liquid
Increasing
cooling rate
3
2
1
Glasses obtained at different cooling rates have different structures
With increasing cooling rate:
V1 < V2 < V3
Free volume increases
H1 < H2 < H3
Configurational entropy increases
Tf,1 < Tf,2 < Tf,3

## Slide 25: Glass formation from liquid
V
T
Tm
Supercooled liquid
Liquid
The heating curve never retraces the cooling curve during glass transition due to structural relaxation

## Slide 26: What is amorphous solid (glass)?
A metastable solid with no long-range atomic order (and exhibiting glass transition)
Liquid: atoms do not have fixed positions; bonding constraints relax as temperature rises
Crystal: atoms arranged with both short range and long range order
Glass: atoms arranged with short range order but lack long range order
Solidification
Melting
Melt quenching
Softening
Crystallization
Amorphization (vitrification)

## Slide 27: What is amorphous solid (glass)?
A metastable solid with no long-range atomic order (and exhibiting glass transition)
Normalized distribution
Si-O-Si bond angle in fused silica
Si-O-Si bond-bending constraint is relaxed at the forming temperature of silica glass
Si-O-Si bond angle distribution in silica glass measured by XRD
J. Appl. Cryst. 2, 164 (1969)
144°: Si-O-Si bond angle in a-quartz

## Slide 28: Quantitative description of glass structure
Structural descriptions of amorphous materials are always statistical in nature
Pair distribution function (PDF): g(r)
  Consider an amorphous material with an average number density of atom given by:
  The number density of atoms at a distance r from an origin atom is given by
  When
  When
n : number of atoms V : material volume

## Slide 29: PDFs of ideal (hard sphere) crystals vs. glasses
g(r)
r
1st coordination shell
2nd coordination shell
g(r)
r
1
0

## Slide 30: Quantitative description of glass structure
Pair correlation function h(r)
Radial distribution function (RDF): J(r)
  J(r)dr gives the number of atoms located between r and r + dr away from the origin atom
  The area under the RDF curve gives the number of atoms
Reduced radial distribution function (rRDF): G(r)
Notes: Beware that different books may use different terminologies

## Slide 31: Summary
The amorphous state is metastable
Amorphous structures possess short-range order and lack long-range order
Amorphous materials can be obtained from liquid by melt quench
Melt quench is a continuous, irreversible process involving phase change
Glass properties depend on their thermal history
V
T
Tm
Supercooled liquid
Liquid
Glass
Crystal

## Slide 32: Crystalline vs. amorphous

## Slide 33: Crystalline vs. amorphous

## Slide 34: After-class reading list
Fundamentals of Inorganic Glasses
  Ch. 1 & 2
Introduction to Glass Science and Technology
  Ch. 1