## Slide 1: MIT 3.071 Amorphous Materials 10: Metallic Glass
Juejun (JJ) Hu
hujuejun@mit.edu

## Slide 2: After-class reading list
Structure of metallic glass
  D. Miracle, “A structural model for metallic glasses”
Mechanical properties
  C. Schuh et al., “Mechanical behavior of amorphous alloys”
Topical review
  M. Chen, “A brief overview of bulk metallic glasses”

## Slide 3: Metallic glass: the timeline
1960: First report of a metallic glass in binary Au-Si via rapid solidification (RS)
1970’s: Study of RS ribbons; commercialization in magnetic applications
1980’s: First observation of ‘bulk’ metallic glass (BMG) formers > 1 mm in size
1990’s: Development of ‘cheap’ bulk glasses (Vitreloy) based on Zr
2000’s: First limited commercialization of BMG, rapid increase in number of glass forming alloys, discovery of bulk binary glasses
2010’s: Gradual increase in understanding toughness and plasticity

## Slide 4: Metallic glass: the timeline
Mater. Trans. 43, 1892 (2002)

## Slide 5: Metallic glass: structure
Polycrystalline metal
Amorphous metal
Metallic bonding, largely non-directional, is mostly about achieving dense packing
Notes: It is frequently presumed that free volume (similar to Fictive temperature in network glasses) is an adequate state variable to describe the structure of a metallic glass, although it is important to remember that other effects such as chemical ordering may be involved.

## Slide 6: Metallic glass: structure
Polycrystalline metal
Amorphous metal
Inoue’s empirical rules for bulk metallic glass (BMG) formation
  Multicomponent systems consisting of three or more elements
  Significant difference in atomic size ratios (frustration)
  Negative enthalpy of mixing

## Slide 7: 3D atomic structure of a multi-component metallic glass nanoparticle
Close-packed structure imaged using atomic electron tomography
Nature 592, 60-64 (2021)

## Slide 8: Hard sphere packing in 2-D
Philos. Mag. 83, 2409 (2003)
Dense packing is only achieved at certain critical radius ratios

## Slide 9: Hard sphere packing in 3-D
Philos. Mag. 83, 2409 (2003)
Local structures of metallic glasses are efficiently packed in systems with critical atomic radius ratios
Notes: The discontinuity results from a transition from substitutional to interstitial structure

## Slide 10: Dense packing favors metallic glass formation
Philos. Mag. 83, 2409 (2003)
Stable binary metallic glasses tend to form at atomic size ratios corresponding to dense packing
Notes: Histogram of atomic radius ratios in known stable binary metallic glasses
Coordination number 12 corresponds to regular close packed structures and has minimal probability

## Slide 11: Beyond nearest neighbors: cluster packing
Close-packed clusters sharing faces or edges
Atoms of different critical sizes fulfill different topological roles
a: center atom of polyhedral; b / g: filling in interstitials
Nat. Mater. 3, 697 (2004)
Notes: Although metallic glasses can have any number of chemically distinct solute species, this model shows that they contain no more than three topologically distinct solutes and that these solutes have specific and predictable sizes relative to the solvent atoms.
alpha: cluster forming solute; beta/gamma: secondary/tertiary solutes filling in octahedral/tetrahedral interstices

## Slide 12: Beyond nearest neighbors: cluster packing
The cluster packing model correctly predicts the atomic size and concentration of stable metallic glasses
D. Miracle, Nat. Mater. 3, 697 (2004)
Notes: Elements enclosed in parentheses in the legends have nearly identical atomic radii and thus represent topologically identical solutes

## Slide 13: Mechanical properties of metallic glasses
Absence of dislocations and slip planes/directions in BMG
  Large elastic limit and high yield strength (2% and 2 GPa in Zr-based BMGs)
  Poor global plasticity: absence of strain hardening, strong tendency towards shear localization
Polycrystalline metal
Amorphous metal
Grain boundaries
Crystal planes
Metals 3, 1 (2013)

## Slide 14: A deformation map of metallic glasses
Schuh et al., Acta Mater. 55, 4067 (2007)
Shear localization at high stresses

## Slide 15: A deformation map of metallic glasses
Schuh et al., Acta Mater. 55, 4067 (2007)
Scr. Mater. 39, 301 (1998)
Homogeneous flow at high temperatures
Notes: Photograph of Pd40Ni40P20 metallic glass before and after the deformation to 1260% at an initial strain rate of 1.7 × 10−1 s−1 and at 620 K

## Slide 16: Elastic and anelastic deformation
Isotropic media
Bulk modulus: typically ~ 6% smaller than that of the crystalline counterpart
  Can be accounted for by the less dense packing (presence of free volume) in metallic glasses
Shear/Young’s modulus: ~ 30% smaller than that of the crystalline counterpart
  In a crystal, all atoms undergo similar displacement defined by the macroscopic strain
  In metallic glass, non-uniform local displacement takes place, e.g. through STZ

## Slide 17: Atomistic mechanisms of deformation
Acta Mater. 55, 4067 (2007)
Diffusive atomic jump
Shear transformation zone (STZ)
Notes: Both mechanisms strongly correlate with local distributions of free volume.
STZs comprise a few to perhaps 100 atoms. An STZ is not a structural defect in an amorphous metal in the way that a lattice dislocation is a crystal defect. Rather, an STZ is an event defined in a local volume, not a feature of the glass structure.

## Slide 18: Atomistic origin of plastic deformation
t
“The plastic deformation of metallic glasses on the macroscopic scale is essentially a biased accumulation of local strains incurred through the operation of STZs and the redistribution of free volume.”
Image courtesy of C. Schuh
Schuh et al., Acta Mater. 55, 4067 (2007)

## Slide 19: Atomistic origin of plastic deformation
Image courtesy of C. Schuh
t
Once a local deformation occurs in a STZ, its surrounding regions are placed under strain
The strain catalyzes plastic deformation in surrounding STZs
STZs “talk” with each other through strain
Phys. Rev. B 81, 064204 (2010)

## Slide 20: The origin of shear localization
Strain softening
Homogeneous deformation: at high temperatures, all zones readily deform
Shear localization: STZs adjacent to the one that has already deformed preferentially deforms due to strain coupling; this effect is most pronounced at high stress levels and reduced temperatures
Kinetic Monte Carlo modeling of STZs
Acta Mater. 57, 2823-2833 (2009)

## Slide 21: Shear localization and shear band formation
J. Appl. Phys. 94, 904 (2003); Nat. Mater. 5, 15 (2006)
Plastic strain concentrated in narrow shear bands in both compressive and tensile regions

## Slide 22: Shear deformation in metallic glass is dilatational
Free-volume creation: strain softening
Shear deformation is a pressure-dependent, frictional process

## Slide 23: Shear angles in uniaxial loading tests
Intermetallics 10, 1071-1077 (2002)
Fractured surface in tensile test
Fractured surface in compressive test

## Slide 24: Shear angles in uniaxial loading tests
Acta Mater. 51, 5399-5411 (2003)
Shear angles are larger than 45° in tension and smaller than 45° in compression

## Slide 25: Tensile/compression asymmetry due to friction
Acta Mater. 51, 5399 (2003)
Metallic glass is stronger in compression than in tension
CuCr metallic glass simulation
20% strength difference
Notes: Vertical axis is normal stress normalized by Young’s modulus

## Slide 26: Summary
Metallic glass structure is dictated by close packing requirements
Large elastic limit, lower elastic moduli compared to crystalline metals
Plastic deformation
  Homogeneous flow (important for thermoplastic forming): high temperature
  Inhomogeneous deformation (strain softening): high stress
Atomistic mechanisms of plastic deformation
  Shear transformation zone and STZ coupling
  Pressure-dependent, frictional shear deformation