## Slide 1: MIT 3.156/3.46 Photonic Materials and Devices 15: Flat Optics
Juejun (JJ) Hu
hujuejun@mit.edu

## Slide 2: References
“A review of metasurfaces: physics and applications,” Rep. Prog. Phys. 79, 076401 (2016).
“Advances in optical metalenses,” Nat. Photonics 17, 16 (2023).

## Slide 3: Flat optics: how it works
Micro-structures
Phase delay
x
Phase delay
x
Focal spot
Wavefront

## Slide 4: Phase wrapping
Represent the optical phase profile as modulo 2p
The positions of the Fresnel zone boundaries are wavelength-dependent
Unwrapped phase
Wrapped phase
Fresnel zone
Optical micrograph of a flat lens showing the Fresnel zones

## Slide 5: Fresnel lens
Removes non-refractive parts of a traditional lens
Thin profile for weight reduction
Fresnel lens at Boston Light
https://www.insidescience.org/news/remarkable-lens-americas-oldest-lighthouse-station

## Slide 6: Diffractive optical element (DOE)
Generating optical phase delay by varying height
J. Infrared, Millimeter, Terahertz Waves 40, 477 (2019)
Multi-level DOE

## Slide 7: Binary multi-level DOEs
n binary masks needed to produce 2n different levels
Optical efficiency depends on the phase accuracy
Diffraction efficiencies of DOEs
  2n = 2: up to 41%
  2n = 4: up to 81%
  2n = 8: up to 95%
IEEE Trans. THz Sci. Technol. 3, 479-485 (2013)

## Slide 8: Optical metasurfaces
Science, 334, 333 (2011)
Plasmonic metal antennas
Phase delay
x
Meta-atoms
Dx < l
Eliminating spurious diffraction orders

## Slide 9: Optical metasurfaces
Opt. Lett. 23, 1081 (1998)
Nat. Nanotechnol. 10, 937 (2015)
Science 352, 1190 (2016)
Nat. Commun. 5, 5753 (2014)
ACS Photonics 3, 209 (2016)
Nano Lett. 15, 6261 (2015)
and many others
…

## Slide 10: Optical phase modulation mechanisms
Resonator
Waveguide
Nat. Photonics 14, 498 (2020)
Adv. Opt. Mater. 3, 813 (2015)
Pancharatnam-Berry phase
Adv. Opt. Mater. 5, 1700040 (2017)

## Slide 11: Waveguide-type meta-atoms
Nano Lett. 23, 51 (2023)
a-Si
SiO2
Each meta-atom acts as a truncated waveguide to impart optical phase delay to the incident lightwave
Solving the meta-atom optical response assuming periodic boundary condition
Guided mode resonances

## Slide 12: Resonance and phase delay
Wavelength
Transmittance / Phase (2p)
Critically coupled resonator

## Slide 13: Resonance and phase delay
Wavelength
Transmittance / Phase (2p)
Under coupled resonator

## Slide 14: Resonance and phase delay
Wavelength
Transmittance / Phase (2p)
Over coupled resonator

## Slide 15: Resonance and phase delay
Wavelength
Transmittance / Phase (2p)
Heavily over coupled resonator

## Slide 16: Dielectric Huygens metasurface
Adv. Opt. Mater. 3, 813 (2015)
Kerker condition: suppression of back scattering

## Slide 17: Pancharatnam-Berry (geometric) phase
Extra phase delay acquired by light due to change of its polarization state
Operates with circularly polarized light
Light Sci. Appl. 8, 92 (2019)
Phase-gradient metasurface implemented with anisotropic meta-atoms with spatially varying orientations

## Slide 18: Multi-level DOEs vs. metasurfaces
Low lithographic resolution requirement
Ease of achieving high efficiency at small angles
Multiple patterning steps involved
Efficiency limitations due to shadowing and spurious diffraction orders
Polarization insensitivity
Fine-line patterning methods required
Extensive optimization needed to achieve high efficiency
Single mask level lithography
Capable of large light bending angles
Polarization manipulation capability
Nat. Commun. 11, 1991 (2020)

## Slide 19: Advantages and limitations of flat optics
System-level Size, Weight and Power (SWaP) benefits
Simplified packaging
Wafer-level integration compatibility
Low monochromatic aberration
Low fabrication cost at high volume
Polarization discrimination capacity
Chromatic aberration
Moderate efficiency

## Slide 20: Flat optics functions
Nat. Photonics 17, 26 (2023)

## Slide 21: Compact, wide field-of-view optics: an unmet need
Fisheye-Nikkor 6 mm f/2.8
Wide field-of-view optics are vital for imaging, sensing, and display
Conventional wide-angle optical systems are bulky and complicated

## Slide 22: A single-element, flat fisheye metalens
Ultra-wide FOV: unprecedented near-180° FOV
High resolution: diffraction-limited performance across the entire FOV
Compact, light-weight, and low-cost optics compatible with standard silicon foundry manufacturing
Nano Lett. 20, 7429-7437 (2020)

## Slide 23: Foundry fabricated fisheye metalens
200 mm metalens wafer
Scalable manufacturing of wide-FOV metalenses on 200 mm glass wafers leveraging commercial foundry process

## Slide 24: A fisheye meta-camera
Circular 180° target
Metalens + image sensor assembly
Camera position

## Slide 25
Diffraction-limited performance across 180° FOV

## Slide 26: Applications
Near-eye display
Night vision
LiDAR
Medical imaging
Flat optics
Sensing and tracking

## Slide 27: 3-D optical sensing: state-of-the-art
Structured light 3-D scanner
Conventional 3-D sensor optics modules
FOV typically < 90°
Bulky
Poor resolution
Complex assembly

## Slide 28: 3-D optical sensing: state-of-the-art
Source: System Plus Consulting
Structured light 3-D scanner
Conventional 3-D sensor optics modules
Field-of-view typically < 90°
Bulky
Poor resolution
Complex assembly

## Slide 29: Metasurface projection optics
Nano Lett. 20, 6719 (2020)
Nat. Commun. 20, 6719 (2023)
SPIE Proc. PC12432, 0Q (2023)
Structured light
Beam steering
High resolution, large field-of-view, high contrast
Projection display
Holography

## Slide 30: Metasurface-enabled 3-D sensor
An all-planar, high-performance 3-D sensor for integration with mobile devices, AR/VR modules, automobile systems, robotics, etc.

## Slide 31: Metasurface color routers
Nano Lett. 17, 6345 (2017); Optica 8, 1596 (2021)
Reduce photon loss due to filtering

## Slide 32: List of symbols
h – diffraction efficiency
Dj – average optical phase error