## Slide 1: MIT 3.156/3.46 Photonic Materials and Devices 3: Guided Wave Optics
Juejun (JJ) Hu
hujuejun@mit.edu

## Slide 2: Guided wave optics vs. multi-layers
Longitudinal variation of refractive indices
  Refractive indices vary along the light propagation direction
  Approach: transfer matrix method
  Devices: DBRs, ARCs
Transverse variation of refractive indices
  The index distribution is not a function of z (light propagation direction)
  Approach: guided wave optics
  Devices: fibers, planar waveguides
H
L
H
L
H
L
High-index substrate
Light

## Slide 3: Why is guided wave optics important?
It is the very basis of numerous photonic devices
  Optical fibers, waveguides, traveling wave resonators, waveguide lasers, waveguide modulators…
Fiber optics
The masters of light
“If we were to unravel all of the glass fibers that wind around the globe, we would get a single thread over one billion kilometers long – which is enough to encircle the globe more than 25 000 times – and is increasing by thousands of kilometers every hour.”
-- 2009 Nobel Prize in Physics
Press Release

## Slide 4: Waveguide geometries and terminologies
Slab waveguide
Channel/photonic wire
waveguide
nhigh
nlow
nlow
nhigh
nlow
Rib/ridge waveguide
nhigh
nlow
nlow
1-d optical confinement
2-d optical confinement
cladding
cladding
core
core
cladding
Step-index fiber
Graded-index (GRIN) fiber
core
cladding

## Slide 5: How does light propagate in a waveguide?
light
?
Question:
If we send light through a channel waveguide, what are we going to see at the waveguide output facet?
JJ knows the answer, but we don’t !
A
B
C
D
E

## Slide 6: Modes
“When asked, many well-trained scientists and engineers will say that they understand what a mode is, but will be unable to define the idea of modes and will also be unable to remember where they learned the idea!”
Quantum Mechanics for Scientists and Engineers
David A. B. Miller

## Slide 7: What is a waveguide mode?
A propagation mode of a waveguide at a given wavelength is a stable cross-sectional shape (complex amplitude of fields) in which the wave propagates
Waveguide modes at any given wavelength are completely determined by the cross-sectional geometry and refractive index profile of the waveguide
Si
SiO2
500 nm
220 nm
z
y
x
Fundamental TE mode @ 1550 nm
1
0

## Slide 8: What is a waveguide mode?
A propagation mode of a waveguide at a given wavelength is a stable cross-sectional shape (complex amplitude of fields) in which the wave propagates
Waveguide modes at any given wavelength are completely determined by the cross-sectional geometry and refractive index profile of the waveguide
Si
SiO2
x
z
y

## Slide 9: 1-d optical confinement: slab waveguide
Wave equation:
with spatially non-uniform refractive index
z
y
x
Helmholtz equation:
k = nk0 = nω/c0
Propagation constant: β = neff k0
Propagation constant is related to the wavelength (spatial period) of light propagating in the waveguide
effective index
z
Field boundary conditions
TE: E-field parallel to substrate

## Slide 10: Quantum mechanics = Guided wave optics
?
"According to the experiment, grad students exist in a state of both productivity and unproductivity."
Quantum mechanics
Guided wave optics
-- Ph.D. Comics
“The equations for many different physical situations have exactly the same appearance… (therefore) it is actually quite possible for a physicist to retain a broad knowledge of the physical world rather than to become a specialist in some narrow area.”
-- R. P. Feynman

## Slide 11: Quantum mechanics = Guided wave optics
?
Quantum mechanics
1-d time-independent Schrödinger equation
ψ(x) : time-independent wave function (time cross-section)
-V(x) : potential energy landscape
-E : energy (eigenvalue)
Time-dependent wave function (energy eigenstate)
t : time evolution
Guided wave optics
Helmholtz equation in a slab waveguide
U(x) : cross-sectional optical mode profile (complex amplitude)
k02n(x)2 : x-sectional index profile
β2 : propagation constant
Electric field along z direction (waveguide mode)
z : wave propagation
“The equations for many different physical situations have exactly the same appearance… (therefore) it is actually quite possible for a physicist to retain a broad knowledge of the physical world rather than to become a specialist in some narrow area.”
-- R. P. Feynman

## Slide 12: Slab waveguide in a quantum mechanics lens
Helmholtz equation:
x
n
ncore
nclad
ncore
nclad
nclad
Schrödinger equation:
?
V
x
V0
Vwell
1-d potential well (particle in a well)
E1
E2
E3
Discretized energy levels (states)
Wave functions with higher energy have more nodes (ψ = 0)
Deeper and wider potential wells gives more bounded states
Bounded states: Vwell < E < V0
Discretized propagation constant β values
Higher order mode with smaller β have more nodes (U = 0)
Larger waveguides with higher index contrast supports more modes
Guided modes: nclad < neff < ncore

## Slide 13: Waveguide dispersion
At long wavelength, effective index is small (QM analogy: reduced potential well depth)
At short wavelength, effective index is large
ncore
nclad
nclad
short λ
high ω
long λ
low ω
ncoreω/c0
ncladω/c0
waveguide dispersion
β = neff k0 = neff ω/c0

## Slide 14: Group velocity in waveguides
ncoreω/c0
ncladω/c0
Low vg
Group velocity vg: velocity of wave packets (information)
Phase velocity vp: traveling speed of any given phase of the wave
Effective index: spatial periodicity (phase)
  Waveguide effective index is always smaller than core index
Group index: information velocity (wave packet)
  In waveguides, group index can be greater than core index!
Group index

## Slide 15: 2-d confinement: effective index method (EIM)
Channel waveguide
ncore
nclad
Rib/ridge waveguide
ncore
nclad
nclad
Directly solving 2-d Helmholtz equation for U(x,y)
Deconvoluting the 2-d equation into two 1-d problems
  Separation of variables
  Solve for U’(x) & U”(y)
  U(x,y) ~ U’(x) U”(y)
Less accurate for high-index-contrast waveguide systems
neff,core
nclad
nclad
neff,core
neff,clad
neff,clad
y
x
z
EIM mode solver:
http://www.computational-photonics.eu/eims.html

## Slide 16: Guided modes in a channel waveguide
Ex
Ey
Ez
Ex
Ey
Ez
(Quasi-)TE
(Quasi-)TM
For channel waveguides, all six E/H field components are non-zero!
z
y
x

## Slide 17: Guided modes in a channel waveguide
Each mode has different effective and group indices
Single-mode (only fundamental TE and TM modes are supported) waveguides are preferred in most applications
Fundamental
Fundamental
2nd order
2nd order
TE
TM
TE 2nd order
TE fundamental
TM fundamental
TM 2nd order
Notes: Mode profiles at 1550 nm wavelength

## Slide 18: Coupled waveguides and supermodes
supermodes
WG 1
WG 2
Cladding
V
y
Modal overlap!
neff + Δn
neff - Δn
z
y
x
Anti-symmetric
Symmetric
y

## Slide 19: Waveguide directional coupler
F+
F-
Input 1
Input 2
Output 1
Output 2
s0
Field at input (z = 0)
Field at output z > 0
When
sz

## Slide 20: Waveguide directional coupler
F+
F-
Input 1
Input 2
Output 1
Output 2
s0
Field at input (z = 0)
Field at output z > 0
When
sz

## Slide 21: Waveguide directional coupler
Optical power
Propagation distance
Beating length
Optical power
Propagation distance
WG 1
WG 2
Cladding
Asymmetric waveguide directional coupler
Symmetric coupler
3 dB direction coupler

## Slide 22: Beating in a directional coupler
Asymmetric directional coupler
Symmetric directional coupler

## Slide 23: Optical loss in waveguides
Material attenuation
  Electronic absorption (band-to-band transition)
  Bond vibrational (phonon) absorption
  Impurity absorption
  Semiconductors: free carrier absorption (FCA)
  Glasses: Rayleigh scattering, Urbach band tail states
Roughness scattering
  Planar waveguides: line edge roughness due to imperfect lithography and pattern transfer
  Fibers: frozen-in surface capillary waves
Optical leakage (imperfect waveguiding)
  Bending loss
  Substrate leakage

## Slide 24: Waveguide confinement factor
core
cladding
A waveguide consists of an absorptive core with an absorption coefficient acore and an non-absorptive cladding. How do the mode profile evolve when it propagate along the guide?
x
E
Propagation
?
E
x
Confinement factor:
Modal attenuation coefficient:
J. Robinson, K. Preston, O. Painter, M. Lipson, "First-principle derivation of gain in high-index-contrast waveguides," Opt. Express 16, 16659 (2008).
Note that in general

## Slide 25: Absorption in silica (glass) and silicon (semiconductor)
Short wavelength edge: Rayleigh scattering (density fluctuation in glasses)
Long wavelength edge: Si-O bond phonon absorption
Other mechanisms: impurities, band tail states
Short wavelength edge: band-to-band transition
Long wavelength edge: Si-Si phonon absorption
Other mechanisms: FCA, oxygen impurities (the arrows below)

## Slide 26: Roughness scattering
Origin of roughness:
  Planar waveguides: line edge roughness evolution in processing
    T. Barwicz and H. Smith, “Evolution of line-edge roughness during fabrication of high-index-contrast microphotonic devices,” J. Vac. Sci. Technol. B 21, 2892-2896 (2003).
  Fibers: frozen-in capillary waves due to energy equi-partition
    P. Roberts et al., “Ultimate low loss of hollow-core photonic crystal fibres,” Opt. Express 13, 236-244 (2005).
QM analogy: time-dependent perturbation
Modeling of scattering loss
  High-index-contrast waveguides suffer from high scattering loss
  F. Payne and J. Lacey, “A theoretical analysis of scattering loss from planar optical waveguides,” Opt. Quantum Electron. 26, 977 (1994).
  D. Kita, J. Michon, S. G. Johnson, and J. Hu, "Are slot and sub-wavelength grating waveguides better than strip waveguides for sensing?" Optica 5, 1046-1054 (2018).
where s is the RMS roughness

## Slide 27: Optical leakage loss
Single-crystal
Silicon
Silicon oxide cladding
Silicon substrate
x
x
n
nSi
nSiO2
V
x
QM analogy
Tunneling!
Unfortunately quantum tunneling does not work for cars!

## Slide 28: Waveguide bending loss
Radiative bending loss
  Guided modes in a bent waveguide are inherently lossy (leaky)
Junction loss
  Mismatch between modes of a straight and a bent waveguide sections
  Mitigation: use a bend design with smoothly changing curvature (e.g. Bezier curve, Euler spiral)
Radiative bending loss
Scattering loss at junctions
Example: Light Sci. Appl. 7, e17138 (2018)

## Slide 29: Waveguide bending loss
High index contrast (core-cladding index difference) enables small bending radius
5 mm
50 mm
Image from EPFL
Doped silica (n ~ 1.5), bending radius ~ mm
SiNx (n ~ 2.0), bending radius ~ 20 mm
Si (n = 3.5), bending radius < 5 mm
J. Lightwave Technol. 33, 3116 (2015)
1 mm

## Slide 30: Waveguide loss measurement
Cut-back
Camera imaging
Ring resonator
Fabry-Perot

## Slide 31: Waveguide loss measurement
Cut-back
Camera imaging
Ring resonator
Fabry-Perot
Waveguide length
Transmitted power (in dB)

## Slide 32: Waveguide loss measurement
Cut-back
Camera imaging
Ring resonator
Fabry-Perot
Waveguide length
Transmitted power (in dB)

## Slide 33: Waveguide loss measurement
Cut-back
Camera imaging
Ring resonator
Fabry-Perot
Waveguide length
Transmitted power (in dB)

## Slide 34: Waveguide loss measurement
Cut-back
Camera imaging
Ring resonator
Fabry-Perot
Waveguide length
Transmitted power (in dB)
Slope: propagation loss
Intercept: coupling loss

## Slide 35: Waveguide loss measurement
Cut-back
Camera imaging
Ring resonator
Fabry-Perot
Waveguide “paperclips” for cutback measurement
Sensitivity to facet quality

## Slide 36: Waveguide loss measurement
Cut-back
Camera imaging
Ring resonator
Fabry-Perot
Appl. Opt. 22, 3892-3894 (1983)

## Slide 37: Waveguide loss measurement
Cut-back
Camera imaging
Ring resonator
Fabry-Perot
Appl. Opt. 22, 3892-3894 (1983)
Sensitivity to defects and surface quality

## Slide 38: Boundary conditions
Guided wave optics
Quantum mechanics
Continuity of wave function
Continuity of the first order derivative of wave function
Polarization dependent!
x
z
Cladding
Core
Substrate
y
TE mode: Ez = 0 (slab), Ex >> Ey (channel)
TM mode: Hz = 0 (slab), Ey >> Ex (channel)

## Slide 39: Boundary conditions
TE mode profile
Polarization dependent!
x
z
Cladding
Core
Substrate
y
TE mode: Ez = 0 (slab), Ex >> Ey (channel)
TM mode: Hz = 0 (slab), Ey >> Ex (channel)
Guided wave optics
Notes: Unlike in slab waveguide modes, channel waveguide modes have all six non-vanishing field components

## Slide 40
Ex amplitude of TE mode
x
z
y
Discontinuity of field due to boundary condition!
x
y

## Slide 41: Slot waveguides Field concentration in low index material
Cladding
Substrate
x
z
y
TE mode profile
slot
V. Almeida et al., “Guiding and confining light in void nanostructure,” Opt. Lett. 29, 1209-1211 (2004).
Use low index material for:
Light emission
Light modulation
Plasmonic waveguiding

## Slide 42: Resources: VM-Lab Simulations
Waveguide mode 1: fields
Waveguide mode 2: waveguide geometry
Directional coupler

## Slide 43: List of symbols
E – electric field or particle energy depending on context
n – refractive index
c0 – speed of light in vacuum (2.99792458 × 108 m/s)
t – time
b – propagation constant
w – angular frequency
l – wavelength of light
k0 – wave number in free space
neff – waveguide effective index
V – potential energy

## Slide 44: List of symbols
m – mass
ћ – reduced Planck constant (1.055 × 10-34 J·s)
ncore / nclad – refractive index of waveguide core / cladding
ng – waveguide group index
vg – group velocity
vp – phase velocity
acore / awg / awg,s – loss coefficient of core material / waveguide / waveguide due to scattering loss
Gcore / Gclad – confinement factor in core / cladding
e0 – vacuum permittivity (8.854 × 10−12 C/Vm)
H – magnetic field